## Slide 1
PR-Vortrag
Carrie Yan
02.08 2016
Influences of Parameters on Defects of Asymmetrical Roll Forming
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 1

## Slide 2: Outline
Investigation on Twist
Units & Abbreviations
Explanation of Defects
Numerical Model & Measurements of Defects
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 2
Investigation on Curving
Conclusion and Outlook

## Slide 3: Introduction
Roll Forming: continuously transversal bending a long metal strip into constant, desirable cross-sectional profile
Efficient and Effective in mass production for metals
When deforming, only deformations in transversal direction are necessary
Reluctant strains result in unexpected deformations
Unexpected deformations over the elastic range cause permanent defects, such as curving, twist, spring-back
Especially for asymmetrical profile, the sheet undergoes non-uniform bending forces
Previous research has been done on
—pertinent methods to reduce the defects for asymmetrical profile (Ona & Jimma 1983)
—influences factors for symmetrical profiles (Safdarian et al, 2015)
Lack of research on the reason of defects and the influence factors for asymmetrical profiles
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 3

## Slide 4: Units and Abbreviations
MPA Units: mm in length, s in time, MPa in pressure
Abbreviations
S: short flange length (mm)
W: web length of the desired cross section (mm)
T: thickness of the sheet (mm)
F: fillet radius of the top rolls (mm)
HC: Horizontal Curving VC: Vertical Curving
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 4

## Slide 5: Influence Factors
Short Flange and Long Flange Ratio
Length of Web: 40mm or 80mm
Thickness of the flat sheet: 1mm or 2mm
Radius of the fillet of the top rolls: 3mm or 6mm
short flange (mm) | 15 | 25 | 35
Long Flange(mm) | 77 | 67 | 57
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 5

## Slide 6: Numerical Model
① flat sheet:
leftmost bottom node on web section fixed at (0,0) in x-y plane, marked as
thickness × width × length(1002mm)
initial position -100mm in z-direction
② 6 roll stations:
distance between stands 400mm
radius & center of roll
first stand location in z-direction
③ supporting rolls:
located at negative 400mm in z-direction
no deforming forces, only supportive in y-direction
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 6
Fig· Numerical Model
Fig· Front View of Sheet for S35T40T2 at t=0s
△
△

## Slide 7: Setting for simulations
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 7
Material Properties ZstE500
Young ´s Modulus 210000 MPa =2.1×105MPa
Poisson ratio 0.29
Plastic Behavior
Contact Body & Table
flat sheet deformable
rolls rigid: translate 100mm/s in negative z
all touching
Boundary Conditions
I· center of sheet front-end fixed x-direction in the first 5s
II· center of sheet back-end fixed all directions in the simulation
Job Setting
stepping multicriteria
save data every 0.5s
Fig· Plastic Behavior for ZstE500

## Slide 8: Measurements of Defects
Curving:
defined by translation of the centroid of the cross-section along the channel horizontally or vertically
measured by coordinate differences of central nodes locating on the web section of two cross sections at the same time
horizontal curving positive, when sheet convex in z-x plane; vertical curving positive, when sheet convex in z-y plane
Twist:
defined by rotation about centroid of cross section along the length of sheet
measured by the magnitude of twist angle per meter
positive, when the long flange approaches the short flange
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 8

## Slide 9: Explanation of Defects
Forces on the side rolls
Horizontal Curving & Twist:
—force on long flange occurs before force on short flange
—torsional & horizontal bending moment
Vertical Curving: edges of flanges stretched more than web
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 9
Reference: H. Ona & T. Jimma, 1983, “Experiments into the cold roll-forming of straight asymmetrical channels”
Fig· Force on side rolls

## Slide 10
Fig· Force on side rolls for S35W40T1 profile

## Slide 11: Explanation of Defects
Non-uniform Distribution of Longitudinal Strain on Cross Section
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 10
Fig· Longitudinal Strain Distribution on Cross Section
W40T1
Fig· Longitudinal Strain Distribution on Cross Section
W80T2
1

## Slide 12: Progressive Twist Zone
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 11
Slope of the Web
Progressively Twist Zone: approximately Linearly change of twist region
Fig· Slope of web S15W80T2
Discontinuity of the slope (at 400mm)
Boundary Condition 1 (center of sheet front-end fixed x-direction in the first 5s)
After first 5s, a sudden change in x-direction
Set BC1 lasted 2.5s, the location of discontinuity changes to 150mm
Fig· Slope of web S15W40T2

## Slide 13: Progressive Zones and Magnitude of Twist
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 12
Progressive Twist Zone
Magnitude of Twist (degree per 1000mm)
Tolerance of Twist: 1 degree per 1000mm
Unexpected Results:
Web length=40mm
Short flange=15mm
Choice of Measuring Zone (from/to a specific position on the sheet along length(mm)) |  |  |  |  | 
S15 W80 T2 | S25 W80 T2 | S35 W80 T2 | S15 W40 T2 | S25 W40 T2 | S35 W40 T2
90/330 | 90/330 | 90/330 | 60/210 | 60/210 | 90/330
S15 W80 T1 | S25 W80 T1 | S35 W80 T1 | S15 W40 T1 | S25 W40 T1 | S35 W40 T1
90/330 | 60/210 | 90/330 | 60/180 | Weird behave | 90/210
profile | twist | profile | twist | profile | twist | profile | twist
S15W80T2 | 11.3006 | S15W40T2 | 4.9517 | S15W80T1 | 13.2461 | S15W40T1 | 6.7630
S25W80T2 | 8.0791 | S25W40T2 | 12.5284 | S25W80T1 | 7.8057 | S25W40T1 | 0.2671
S35W80T2 | 3.1807 | S35W40T2 | 7.3903 | S35W80T1 | 3.4236 | S35W40T1 | 1.4859
Tendency
Fig· Tendency of Twist with respect to ratio of flanges
Table· Progressive Twist Zones
Table· Magnitude of Twist

## Slide 14: Effect of Input Parameters on Twist
-twist values are decreasing with increase of ratio of flanges,
except W40T2 grows up first and then drops, and W40T1 decrease first and increase then
-fillet radius has very less influence on the magnitude of twist
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 13
Fig· Tendency of Twist with respect to ratio of flanges
Fig· Tendency of Twist with respect to radius of top rolls fillet

## Slide 15: Effect of Input Parameters on Twist
-twist values are increasing with increase of web length, except S25T2 and S35T2
-twist values are decreasing with increase of thickness, except S25W80, S25W40 and S35W40
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 14
Fig· Tendency of Twist with respect to web length
Fig· Tendency of Twist with respect to thickness of sheet

## Slide 16: Explanation of Unexpected Results
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 15
non-constant longitudinal strain on flange edge (S15)
counterclockwise twist (S25W40T1)
Fig· Flange Edge Longitudinal Strain S15W40T2
Fig· Slope of the Web S25W40T1

## Slide 17: Explanation of Unexpected Results
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 16
constant longitudinal strain on web for web length 80mm
Fig· Cross Section Longitudinal Strain W80T2
Fig· Cross Section Longitudinal Strain W80T1

## Slide 18: Explanation of Unexpected Results
unstable behaviour for web length 40mm
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 17
Fig· Cross Section Longitudinal Strain W40T2
Fig· Cross Section Longitudinal Strain W40T1
1

## Slide 19: Explanation of Unexpected Results
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 18
Deformation Length
bending angle increments ∆θ are 13°, 16°, 18°, 18°, 15°, 10°
distance between stands = 400mm
 | (mm) | minimum deformation length | maximum deformation length | (mm) | minimum deformation length | maximum deformation length
short flange | 15 | 28.0178514522438 | 37.589892258425 | 15 | 39.6232255123179 | 53.160135440008
long flange | 77 | 325.862231739234 | 437.19006088123 | 77 | 460.838787590789 | 618.280113432954
thickness | 2 |  |  | 1 |  | 
short flange | 25 | 60.284817817252 | 80.8805703903395 | 25 | 85.2556069623489 | 114.38239957849
long flange | 67 | 264.490540333536 | 354.851296554862 | 67 | 374.046109259075 | 501.835516213563
thickness | 2 |  |  | 1 |  | 
short flange | 35 | 99.8619417366166 | 133.978854052919 | 35 | 141.226112368835 | 189.474712472843
long flange | 57 | 207.544019427205 | 278.44952145766 | 57 | 293.511567063378 | 393.787089681721
thickness | 2 |  |  | 1 |  | 
Reference: Bhattacharyya et al. 1984, “Prediction of strain development while roll forming fundamental sections, Advanced technology of plasticity“
Table· Deformation Length

## Slide 20: Effect of Input Parameters on Curving
Fig· Tendency of Curving with respect to flange ratios
The magnitude of curving is always around 1mm per 1000mm
not problematic
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 19

## Slide 21: Conclusion & Outlook
02. Aug 2016 | Institut für Produktionstechnik und Umformmaschinen | 20
1. In summary, magnitude of twist decrease when the profile cross-sectional area grows to more symmetry.
—ratio of short flange length to the long flange length increases,
—web length decreases,
—thickness increases.
2. The twist is partially progressive because of the boundary condition I.
3. For S15T2, S15T1 and S25T1 profile, the deformation length is sometimes larger than distance between two neighbour stands, which is problematic.
1. In order to neutralize the effect of boundary condition I, we can implement supportive rolls in both x and y directions
2. Investigation on different type of materials
3. Investigation on simulations with asymmetric fillet radius of top rolls
Conclusion
Outlook

## Slide 22
19. Juli 2016 | Institut für Produktionstechnik und Umformmaschinen | 21
Thank you for your attention!

## Slide 23
Front View of the Sheet after deformation at time t=25s
△
Fig· Front View of Sheet for S35T40T2 at t=25s

## Slide 24: Initial Position of Sheet